## Slide 1: Név
TERPLÁN Zénó Program 2016/2017
Simon Andrea
adjunktus
Műszaki Anyagtudományi Kar, Kerámia és Polimermérnöki Intézet

## Slide 2: TERPLÁN Zénó Program TETRA alprogram szakmai konferencia 2017. szeptember 13-14.
Bevezetés
Kristálymázak
Kísérlet
Eredmények
Konklúzió

## Slide 3: TERPLÁN Zénó Program TETRA alprogram szakmai konferencia 2017. szeptember 13-14.
Máz
Klasszikus: oxidok (hálózatképző, átmeneti, módosító), amorf
Kristálymáz: különleges művészeti máz
  Makrokristályos: szabad szemmel látható kristályok
  Mikrokristályos: matt/opál
Nyitott kérdések
  Szövetszerkezet: kristályok száma, mérete, morfológiája
  Hőkezelés, oxidok hatása
Notes: The type and amount of these crystals are mainly affected by the composition of the glaze, the nucleating agent and the firing parameters. Reproducible production is only possible when the crystallization is well-known and controlled. There are several studies concerning the microstructure characterization of different crystal glazes but less researchers apply image analysis to describe size, shape and number of crystals. Heat treatment cylye needs even 20 hours while in this research it took up only 9-11 hours to present crystals resulting reduced energy consumption. Effect of colouring agents, TiO2 and heating time on the phase composition and microstructure of willemite crystal glazes were investigated and reported. The microstructure of the glazes fired with 2 staged fast firing cycles was examined by XRD, SEM and image analyses. Microstructural and image analysis showed that colouring agents, TiO2 and firing parameters changed the shape, size and number of willemite crystals.

## Slide 4: TERPLÁN Zénó Program TETRA alprogram szakmai konferencia 2017. szeptember 13-14.
Máz megnevezés | B | BT2 | BC | BT2C | BO | BT2O
Alkáli fritt | 51 | 51 | 51 | 51 | 51 | 51
ZnO | 24 | 24 | 24 | 24 | 24 | 24
SiO2 | 24 | 24 | 24 | 24 | 24 | 24
Segédanyagok | 1 | 1 | 1 | 1 | 1 | 1
Szintest | - | - | 2 | 2 | 2 | 2
TiO2 | - | 2 | - | 2 | - | 2
Máz keverék színe | Fehér | Fehér | Fekete | Fekete | Kék | Kék
Kísérletek
 | B | BT2 | BC | BT2C | BO | BT2O
SiO2 | 56,26 | 55,15 | 55,18 | 54,11 | 55,26 | 54,18
ZnO | 24,24 | 23,76 | 23,76 | 23,3 | 23,76 | 23,3
Na2O | 7,64 | 7,49 | 7,49 | 7,34 | 7,49 | 7,34
Al2O3 | 6,7 | 6,57 | 6,58 | 6,45 | 7,88 | 7,73
CaO | 3,72 | 3,65 | 3,65 | 3,58 | 3,65 | 3,58
K2O | 1,1 | 1,08 | 1,08 | 1,06 | 1,08 | 1,06
TiO2 | 0,33 | 2,31 | 0,33 | 2,26 | 0,33 | 2,26
Cr2O3 | 0 | 0 | 0,65 | 0,64 | 0 | 0
Fe2O3 | 0 | 0 | 0,58 | 0,57 | 0 | 0
CoO | 0 | 0 | 0,31 | 0,3 | 0,56 | 0,55
NiO | 0 | 0 | 0,23 | 0,23 | 0 | 0
MnO | 0 | 0 | 0,16 | 0,16 | 0 | 0
OS-205: CoO
CK 13074: CoO, Cr2O3, Fe2O3

## Slide 5: TERPLÁN Zénó Program TETRA alprogram szakmai konferencia 2017. szeptember 13-14.
Notes: . Heat treatment cylye needs even 20 hours while in this research it took up only 9-11 hours to present crystals resulting reduced energy consumption

## Slide 6: TERPLÁN Zénó Program TETRA alprogram szakmai konferencia 2017. szeptember 13-14.
Mikroszerkezet jellemzése: kristályok száma, mérete, morfológiája, hőkezelés, oxidok hatása
Chart: Area, µm2
| B | BT2 | BC | BT2C | BO | BT2O
A | 4.0225 | 11.3124 | 2.1522 | 11.9421 | 11.3516 | 7.9698
II
B | 1.6214 | 2.9783 | 1.9211 | 3.3829 | 1.0132 | 3.2197
Chart: Perimeter, µm
| B | BT2 | BC | BT2C | BO | BT2O
I | 9.6376 | 12.8458 | 5.6282 | 14.8798 | 12.748 | 12.5932
III | 5.8237 | 8.2775 | 5.2801 | 6.9234 | 3.6997 | 7.0808
Chart: Crystal density 1/µm2
| B | BT2 | BC | BT2C | BO | BT2O
A | 27.4998 | 25.2817 | 52.7466 | 10.8242 | 60.9207 | 24.8234
II
B | 88.7101 | 71.2654 | 21.2193 | 126.7516 | 164.6332 | 49.9228
There is contrary information concerning the effect of the coloring oxides. According to references [11, 18], coloring pigments such as Fe2O3, CuO, and MnO have negligible effect on the willemite crystallization i.e. the shape, size, and quantity of crystals formed in firing and change only the background color of the glaze. On the contrary, Karasu et al. [28] showed that incorporating CoO, MnO and CuO as coloring agents to the glaze studied changed the shape of willemite crystals from needle-like to leaves-like ones. Others reported that some oxides, such as CoO, CuO, TiO2 or ZrO2 served as nucleating agents on whose surfaces willemite crystals formed [3, 28, 36, 37].

## Slide 7: TERPLÁN Zénó Program TETRA alprogram szakmai konferencia 2017. szeptember 13-14.
Makroszerkezet jellemzése
  Kristályok színét az összetétel (színtestek), alakját a hőkezelés (hőelvonás, hőmérsékletgradiens) határozza meg
  Erős hőelvonás → „seaweed” (hínár) alak
  B, BT, BT2O minták – kemence szélén
  László Gránásy, Tamás Pusztai, Jack F. Douglas: Insights into Polymer Crystallization from Phase-Field Theory
  DOI 10.1007/978-3-642-37179-0_30-1
  1. típusú szferolit (szálak radiális növekedése): BO minták
  2. típusú szferolit (egyirányú növekedés, kisszögű elágazásokkal): BC, BT2C minták
Firing B
Sample B
Sample BT
Sample BT2O
Sample BO
Firing A
Firing B
Firing B
Sample BC
Sample BT2C

## Slide 8: TERPLÁN Zénó Program TETRA alprogram szakmai konferencia 2017. szeptember 13-14.
Összegzés
Kristálymáz: willemit (ZnO) makrokristályok
Mikroszerkezet
  Kristályok száma: színtest és TiO2 hatására nő (irodalomban ellentétes álláspont)
  Mérete: TiO2, OS 205 színtest, hőntartási idő növeli
Makroszerkezet
  Kristályok színét az összetétel (színtestek), alakját a hőkezelés (hőelvonás, hőmérsékletgradiens) határozza meg → szferolitos vagy dendrites növekedés
Notes: The type and amount of these crystals are mainly affected by the composition of the glaze, the nucleating agent and the firing parameters. Reproducible production is only possible when the crystallization is well-known and controlled. There are several studies concerning the microstructure characterization of different crystal glazes but less researchers apply image analysis to describe size, shape and number of crystals. Heat treatment cylye needs even 20 hours while in this research it took up only 9-11 hours to present crystals resulting reduced energy consumption. Effect of colouring agents, TiO2 and heating time on the phase composition and microstructure of willemite crystal glazes were investigated and reported. The microstructure of the glazes fired with 2 staged fast firing cycles was examined by XRD, SEM and image analyses. Microstructural and image analysis showed that colouring agents, TiO2 and firing parameters changed the shape, size and number of willemite crystals.

## Slide 9: TERPLÁN Zénó Program 2016/2017 Tanévzáró Konferencia
Köszönöm a figyelmet!